Lot Acceptance Report – L10a

STMicroelectronics

Laser Transmitters

Internal Report

D.Bailleux,M.M.Obertino, R.Zuyeuski

Table of Contents

1	Lot Validation Programme	3

1.1	Lot Validation programme workflow	3

2	Technical Validation	4

2.1	Compliance with technical requirements	4

2.2	Validation test results	6

2.2.1 Visual Inspection	6

2.2.2 LIV Characteristics	6

2.2.3 Dynamic Measurement	9

3	Conclusions	12

# Lot Validation Programme

This is an internal lot validation report for the Laser Transmitters (Laserpills) supplied by STMicroelectronics under the terms of CERN Contract F 451/EP/CMS.  We sampled randomly 60 lasers (10% of   total number of lasers of the batch) from lot L10a delivered by ST on September 2003. The validation procedure consisted of evaluation tests described in “Laser Transmitter Quality Assurance Procedure” (Document ID: CMS-TK-QP-0002).

## Lot Validation programme workflow

The lot validation programme flow is shown in Figure 1.  The figure shows the tests to be carried out as described in the test procedure for laserpills (CMS-TK-QP-0002).   The test target specifications are extracted from the technical specification for delivered laserpills (CMS-TK-ES-0004).  All tests were carried out at room temperature.

Figure 1:  Lot Validation testing flow.

Table 1:  ST Serial Numbers of the 60 L10a devices and their correpsonding CMS Serial Numbers

| ST Serial # | CMS Serial # | ST Serial # | CMS Serial # |
| --- | --- | --- | --- |
| XD305A03 XD335C85 XD335C89 XD335C90 XD335C93 XD337C71 XD339C83 XD356C06 XD356C13 XD356C18 XD356C36 XD356C62 XD356C65 XD356C70 XD356C72 XD358C05 XD358C13 XD358C19 XD358C30 XD358C81 XD358C99 XE359C08 XE359C30 XE359C67 XE359C80 XE360C26 XE360C28 XE360C44 XE360C62 XE360C99 | 30201010010209 30201010027480 30201010027788 30201010027871 30201010027858 30201010030913 30201010027686 30201010030835 30201010030698 30201010030158 30201010027481 30201010027396 30201010027417 30201010027329 30201010027493 30201010030692 30201010027420 30201010027377 30201010027312 30201010030580 30201010034868 30201010027043 30201010035965 30201010033030 30201010033258 30201010030300 30201010030313 30201010030755 30201010030403 30201010027707 | XE361C15 XE361C59 XE361C67 XE361C94 XE362C05 XE362C38 XE362C64 XE362C85 XE363C25 XE363C42 XE365C28 XE365C69 XE366C27 XE366C30 XE366C50 XE367C14 XE367C45 XE367C49 XE367C50 XE367C52 XE367C83 XE368C56 XE368C67 XE369C54 XE369C97 XE369C99 XE370C01 XE370C11 XE370C12 | 30201010027881 30201010030868 30201010030710 30201010027428 30201010035970 30201010030418 30201010033942 30201010035989 30201010035802 30201010033489 30201010029661 30201010029378 30201010030762 30201010035923 30201010033081 30201010033304 30201010033014 30201010033155 30201010033431 30201010027246 30201010033318 30201010033354 30201010033127 30201010034825 30201010033310 30201010033427 30201010035832 30201010033469 30201010033402 |

# Technical validation

## Compliance with technical requirements

Table 2 shows the specified performance of the laser transmitters against which the received sample was tested.  The table also gives a summary of the results obtained in comparison with the specifications.

Table 2:  Specification test targets taken from the technical specification.  Cells in gray indicate parameters not measured during qualification.

| # | Specification to be tested | Test Target Specifications | CERN Validation Results |
| --- | --- | --- | --- |
|  |  | Min | Typ | Max | Units | Min | Max | Accepted? |
| 2.2.1 | Number of channels |  | 1 |  |  | 1 | 1 | Yes |
| 2.2.2 | Integral linearity deviation |  |  | 1 | % | 0.06 | 0.63 | Yes |
| 2.2.3 | Tensile load on connector side of pigtail |  |  | 7 | N |  |  |  |
| 2.2.4 | Tensile load on submount side of pigtail | 3 |  |  | N |  |  |  |
| 2.2.5 | Pigtail length Lp |  | 2 |  | m |  |  | Yes |
| 2.2.6 | Size |  |  | 4.5 ( 4 ( 1.35 | mm |  |  | Yes |
| 2.2.21 | Max. input current | 60 | 100 |  | mA | 60 |  | Yes |
| 2.2.22 | Threshold current |  | 5 | 10 | mA | 4.82 | 6.87 | Yes |
| 2.2.23 | Forward voltage |  | 1.2 | 1.75 | V | 1.53 | 1.73 | Yes |
| 2.2.24 | Reverse voltage | 2 |  |  | V |  |  |  |
| 2.2.25 | Rise time |  |  | 0.5 | ns | 0.19 | 0.36 | Yes |
| 2.2.41 | Wavelength | 1285 | 1310 | 1335 | nm |  |  |  |
| 2.2.42 | Fibre output power | 1.3 | 1.6 | 1.9 | mW | 1.319 | 1.899 | Yes |
| 2.2.43 | Slope efficiency | 0.032 | 0.04 | 0.048 | mW/mA | 0.033 | 0.047 | Yes |
| 2.2.44 | RIN |  | -130 |  | dB/Hz |  |  |  |
| 2.2.61 | Magnetic field |  |  | 4 | T |  |  |  |
| 2.2.62 | Hadronic fluence |  |  | 3×1014 | cm-2 |  |  |  |
| 2.2.63 | Gamma radiation dose |  |  | 1.5×105 | Gy(Si) |  |  |  |
| 2.2.64 | Temperature | -20 | -10 | 70 | °C |  |  |  |
| 2.2.65 | Operating humidity |  | Dry N2 flow |  |  |  |  |  |
| 2.2.81 | Optical safety |  | Laser Class 3A |  |  |  |  |  |
| 2.2.82 | Material composition |  | Halogen-free, flame retardant material |  |  |  |  |  |
| others | In-system test |  |  |  |  |  |  |  |

## Validation test results

### Visual Inspection

We did not find any problem for the 60 lasers inspected visually.

### LIV Characteristics

Figure 2, Figure 3 and Figure4 show the results of the LIV measurements performed at CERN. The dashed lines indicate the range or maximum value allowed for each parameter. From the plot is clear that all the lasers met the criteria given in the specifications.

Figure 2: CERN-measured threshold and efficiency for all 60 devices.

Figure 3: CERN-measured forward and fibre output power for all 60 devices.

Figure 4: Maximum value of the integral linearity deviation -measured at CERN for all 60 devices.

Figure 5 and Figure 6 show comparisons between CERN and ST measurements of Ith, Slope Efficiency, Fibre Output Power and Forward Voltage.  The consistency between the two sets of measurements for the slope is good but often the threshold is found bigger by ST than by CERN. Moreover, there is a large spread in the comparison of the forward voltage. Both this effects were already observed before (see Lot Acceptance Report L8) and could be to a difference in the measurements of the optical power and  to the fact that the contact is made with probes in a probe station .

Figure 5: Comparison of CERN-measured Ith and efficiency with the ST measurements. In the histograms on the bottom the ST measurements are plotted in red, the CERN ones in black.

Figure 6: Comparison of CERN-measured Forward Voltage with the ST measurements. In the histograms on the bottom the ST measurements are plotted in red, the CERN ones in black.

### Dynamic Measurement

#### Rise Time

By applying a voltage pulse train to the laser under test it is possible to excite the laser to laser from below threshold.  By observing the resultant optical pulse on an oscilloscope with the aid of an optical probe one can measure the relaxation oscillations of the laser die and thus determine the intrinsic bandwidth of the die without the sub-mount.  A typical optical pulse is shown in Figure 7, while the extracted bandwidth and risetime are shown in Figure 8.

Figure 7 Optical output pulse measured on an oscilloscope using an optical probe.  The laser bandwidth is determined from the relaxation oscillation frequency.

Figure 8: Bandwidth and risetime for 60 devices that were measured at CERN was.   All devices are in spec: bandwidth>1GHz.

# Conclusions

All the 60 lasers sorted randomly from batch L10a were found inside the criteria given in the specification. The lot is therefore accepted.

# Footnotes

Laser Transmitter Quality Assurance Procedure, Version 1.2, 17 January 2003

CMS Tracker Optical Readout Link Specification, Part 2.2: Laser Transmitter, Version 3.5, 14 May 2002