Lot Acceptance Report – L10a

STMicroelectronics

Laser Transmitters

Internal Report

D.Bailleux,M.M.Obertino, R.Zuyeuski

Table of Contents

1	Lot Validation Programme	3

1.1	Lot Validation programme workflow	3

2	Technical Validation	4

2.1	Compliance with technical requirements	4

2.2	Validation test results	6

2.2.1 Visual Inspection	6

2.2.2 LIV Characteristics	6

2.2.3 Dynamic Measurement	9

3	Conclusions	12

# Lot Validation Programme

This is an internal lot validation report for the Laser Transmitters (Laserpills) supplied by STMicroelectronics under the terms of CERN Contract F 451/EP/CMS.  We sampled randomly 60 lasers (10% of   total number of lasers of the batch) from lot L10a delivered by ST on September 2003. The validation procedure consisted of evaluation tests described in “Laser Transmitter Quality Assurance Procedure” (Document ID: CMS-TK-QP-0002).

## Lot Validation programme workflow

The lot validation programme flow is shown in Figure 1.  The figure shows the tests to be carried out as described in the test procedure for laserpills (CMS-TK-QP-0002).   The test target specifications are extracted from the technical specification for delivered laserpills (CMS-TK-ES-0004).  All tests were carried out at room temperature.

Figure 1:  Lot Validation testing flow.

Table 1:  ST Serial Numbers of the 60 L10a devices and their correpsonding CMS Serial Numbers

| ST Serial # | CMS Serial # | ST Serial # | CMS Serial # |
| --- | --- | --- | --- |
| XD305A03. XD335C85. XD335C89. XD335C90. XD335C93. XD337C71. XD339C83. XD356C06. XD356C13. XD356C18. XD356C36. XD356C62. XD356C65. XD356C70. XD356C72. XD358C05. XD358C13. XD358C19. XD358C30. XD358C81. XD358C99. XE359C08. XE359C30. XE359C67. XE359C80. XE360C26. XE360C28. XE360C44. XE360C62. XE360C99. | 30201010010209. 30201010027480. 30201010027788. 30201010027871. 30201010027858. 30201010030913. 30201010027686. 30201010030835. 30201010030698. 30201010030158. 30201010027481. 30201010027396. 30201010027417. 30201010027329. 30201010027493. 30201010030692. 30201010027420. 30201010027377. 30201010027312. 30201010030580. 30201010034868. 30201010027043. 30201010035965. 30201010033030. 30201010033258. 30201010030300. 30201010030313. 30201010030755. 30201010030403. 30201010027707. | XE361C15. XE361C59. XE361C67. XE361C94. XE362C05. XE362C38. XE362C64. XE362C85. XE363C25. XE363C42. XE365C28. XE365C69. XE366C27. XE366C30. XE366C50. XE367C14. XE367C45. XE367C49. XE367C50. XE367C52. XE367C83. XE368C56. XE368C67. XE369C54. XE369C97. XE369C99. XE370C01. XE370C11. XE370C12. | 30201010027881. 30201010030868. 30201010030710. 30201010027428. 30201010035970. 30201010030418. 30201010033942. 30201010035989. 30201010035802. 30201010033489. 30201010029661. 30201010029378. 30201010030762. 30201010035923. 30201010033081. 30201010033304. 30201010033014. 30201010033155. 30201010033431. 30201010027246. 30201010033318. 30201010033354. 30201010033127. 30201010034825. 30201010033310. 30201010033427. 30201010035832. 30201010033469. 30201010033402. |

# Technical validation

## Compliance with technical requirements

Table 2 shows the specified performance of the laser transmitters against which the received sample was tested.  The table also gives a summary of the results obtained in comparison with the specifications.

Table 2:  Specification test targets taken from the technical specification.  Cells in gray indicate parameters not measured during qualification.

| # | Specification to be tested | Test Target Specifications |  |  |  | CERN Validation Results |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Min | Typ | Max | Units | Min | Max | Accepted? |
| 2.2.1 | Number of channels |  | 1 |  |  | 1 | 1 | Yes |
| 2.2.2 | Integral linearity deviation |  |  | 1 | % | 0.06 | 0.63 | Yes |
| 2.2.3 | Tensile load on connector side of pigtail |  |  | 7 | N |  |  |  |
| 2.2.4 | Tensile load on submount side of pigtail | 3 |  |  | N |  |  |  |
| 2.2.5 | Pigtail length Lp |  | 2 |  | m |  |  | Yes |
| 2.2.6 | Size |  |  | 4.5  4  1.35 | mm |  |  | Yes |
| 2.2.21 | Max. input current | 60 | 100 |  | mA | 60 |  | Yes |
| 2.2.22 | Threshold current |  | 5 | 10 | mA | 4.82 | 6.87 | Yes |
| 2.2.23 | Forward voltage |  | 1.2 | 1.75 | V | 1.53 | 1.73 | Yes |
| 2.2.24 | Reverse voltage | 2 |  |  | V |  |  |  |
| 2.2.25 | Rise time |  |  | 0.5 | ns | 0.19 | 0.36 | Yes |
| 2.2.41 | Wavelength | 1285 | 1310 | 1335 | nm |  |  |  |
| 2.2.42 | Fibre output power | 1.3 | 1.6 | 1.9 | mW | 1.319 | 1.899 | Yes |
| 2.2.43 | Slope efficiency | 0.032 | 0.04 | 0.048 | mW/mA | 0.033 | 0.047 | Yes |
| 2.2.44 | RIN |  | -130 |  | dB/Hz |  |  |  |
| 2.2.61 | Magnetic field |  |  | 4 | T |  |  |  |
| 2.2.62 | Hadronic fluence |  |  | 3×1014 | cm-2 |  |  |  |
| 2.2.63 | Gamma radiation dose |  |  | 1.5×105 | Gy(Si) |  |  |  |
| 2.2.64 | Temperature | -20 | -10 | 70 | °C |  |  |  |
| 2.2.65 | Operating humidity |  | Dry N2 flow |  |  |  |  |  |
| 2.2.81 | Optical safety |  | Laser Class 3A |  |  |  |  |  |
| 2.2.82 | Material composition |  | Halogen-free, flame retardant material |  |  |  |  |  |
| others | In-system test |  |  |  |  |  |  |  |

## Validation test results

### Visual Inspection

We did not find any problem for the 60 lasers inspected visually.

### LIV Characteristics

Figure 2, Figure 3 and Figure4 show the results of the LIV measurements performed at CERN. The dashed lines indicate the range or maximum value allowed for each parameter. From the plot is clear that all the lasers met the criteria given in the specifications.

Figure 2: CERN-measured threshold and efficiency for all 60 devices.

Figure 3: CERN-measured forward and fibre output power for all 60 devices.

Figure 4: Maximum value of the integral linearity deviation -measured at CERN for all 60 devices.

Figure 5 and Figure 6 show comparisons between CERN and ST measurements of Ith, Slope Efficiency, Fibre Output Power and Forward Voltage.  The consistency between the two sets of measurements for the slope is good but often the threshold is found bigger by ST than by CERN. Moreover, there is a large spread in the comparison of the forward voltage. Both this effects were already observed before (see Lot Acceptance Report L8) and could be to a difference in the measurements of the optical power and  to the fact that the contact is made with probes in a probe station .

Figure 5: Comparison of CERN-measured Ith and efficiency with the ST measurements. In the histograms on the bottom the ST measurements are plotted in red, the CERN ones in black.

Figure 6: Comparison of CERN-measured Forward Voltage with the ST measurements. In the histograms on the bottom the ST measurements are plotted in red, the CERN ones in black.

### Dynamic Measurement

#### Rise Time

By applying a voltage pulse train to the laser under test it is possible to excite the laser to laser from below threshold.  By observing the resultant optical pulse on an oscilloscope with the aid of an optical probe one can measure the relaxation oscillations of the laser die and thus determine the intrinsic bandwidth of the die without the sub-mount.  A typical optical pulse is shown in Figure 7, while the extracted bandwidth and risetime are shown in Figure 8.

Figure 7 Optical output pulse measured on an oscilloscope using an optical probe.  The laser bandwidth is determined from the relaxation oscillation frequency.

Figure 8: Bandwidth and risetime for 60 devices that were measured at CERN was.   All devices are in spec: bandwidth>1GHz.

# Conclusions

All the 60 lasers sorted randomly from batch L10a were found inside the criteria given in the specification. The lot is therefore accepted.

Laser Transmitter Quality Assurance Procedure, Version 1.2, 17 January 2003

CMS Tracker Optical Readout Link Specification, Part 2.2: Laser Transmitter, Version 3.5, 14 May 2002